****

|  |  |
| --- | --- |
| **PRODUCT****DESCRIPTION** | A phosphoric acid based mordant solution for treating galvanised steelwork. |

|  |  |
| --- | --- |
| **INTENDED USES** | Used in the first stage of a protective coating system on galvanised steel. Techniwash ensures good adhesion between the galvanised zinc layer and the over coating paint. |

|  |  |  |
| --- | --- | --- |
| **PHYSICAL DATA** |  |  |
|  | Colour | Pale Blue |
|  | Gloss Level | N/A |
|  | Volume Solids | N/A |
|  | Flash Point | ≥21˚C & ≤ 35˚C |
|  | Weight (approx) | Base 1.01kg/ltr |
|  | Container Size | 5ltr Base |
|  | Storage Properties | 24 months if base and curing agent are stored separately in original unopened containers.

|  |
| --- |
| . |

 |

|  |  |  |
| --- | --- | --- |
| **APPLICATION DETAILS** |  |  |
|  | Mixing Ratio | N/A |
|  | Induction Period | NIL |
|  | Working Pot Life @ 20˚C | Indefinite |
|  | Surface Preparation | All surfaces to be clean, dry and free from contamination. |
|  | Application | Brush or immersion. |
|  | Recommended Film Thickness | N/A.N/A.  |
|  | Theoretical Spreading Rate | 15 mtrs² per litre \* |
|  | Drying Times | N/A |
|  | Minimum Over Coating | 0˚C = 36hrs, 10˚C =24hrs, 20˚C = 20hrs |
|  | Full Cure | 24 hours @ 10˚C |
|  | Thinners | Water |